## Slide 1
Seyed ali atyabi*, Amin Farkhondehfal, Yuvraj Y. Birdja and Wim De Schepper
*Email:ali.atyabi@vito.be
VITO: Sustainable Chemistry, Flemish Institute for Technological Research, Boeretang 200, 2400, Mol
Symposium on Insights into Gas Diffusion Electrodes: From Fundamentals to Industrial Applications
Magdeburg, Germany,
September 5 – 7, 2022
Conclusion
A numerical model based on the finite element method was used to calculate the effective properties of Nickel foam (porosity=0.95), this one was compared with Bruggeman correlation and catalog details, and there is a good agreement between results and catalog details. The numerical results demonstrate that the developed FEM approach is close to catalog details and the Bruggeman approach.
3D numerical models were used to predict the effective electrical conductivity, permeability, porosity, and Specific active area for 3 different microstructures with changing volume fractions of carbon materials.
The present work indicated that the simple model of microstructure constituted by a cubic matrix and spherical spheres is reliable to predict the effective properties of microstructure, and it gives us an acceptable approximation to the desired results.
Inlet
Outlet
V=0.1 [m/s]
Velocity[m/s]
0
0.1
0.2
0.25
0.05
0.15
:Porosity ; Specific active area [1/m]; K: Permeability [1/m2]
:Effective electrical conductivity[S/m]
Property | Bruggeman | Simulation (Comsol) | Error(%)
 | 5.2e6 | 4.7e6 | 9.6
[S/m]
Properties | Value (simulation) | Value (Catalog) | Error%
Permeability [m2] | 1.648e-9 | - | -
Specific geometrical active area [1/m] | 5227.6 | 5400 | 3.29
References
[1] J. W. Blake, J. T. Padding and J. W. Haverkort, J. Electrochim. Acta, 2021, 393, (2021) 138987
[2] B. J. M. Etzold, U. Krewer, S. Thiele, A. Dreizler, E. Klemm and T. Turek, J. Chem. Eng., 424 (2021), 130501
Figure 3. (a) 3D cell of microstructures, (b) contour of velocity and streamlines, and
(c) contour of electrical current inside the models
Figure 1. (a) 3D numerical model (electrical) of Nickel foam with boundary conditions, (b) contour of current density
Figure 2. (a) 3D numerical model (Fluid dynamic) of Nickel foam with boundary conditions, (b) streamlines of fluid flow
Exportation of models to Comsol
Generation of 3D microstructures
Meshing of models
Applications of boundary conditions
Computing effective properties
Add physics
(electrical current)
Add physics
(Fluid dynamics)
0.965
0.884
0.81
5.95e-3
9.67e-4
3.98e-4
2.1626
7.95
13.695
273.53
575.83
915.43
K
20 m
3D mesh
One ligament of Nickel foam
SEM image
ID46
Introduction
In terms of current density, Gas diffusion electrodes (GDEs) be able to deliver orders of magnitude higher current densities than conventional electrodes for CO2 electrolyzer [1]. The microstructure of an insulating fluid and carbon particles are complex, making it more difficult to predict its properties [2]. The improving configurations of the porous electrode can strongly influence the mass transfer in this Multiphysics system.
Aim of this work
The determination of the effective properties of a GDE microstructure seems very important in the characterization, design, and manufacturing of GDE. In this research, a numerical homogenization technique was used to determine the effective properties of GDE. Thus, 3 different 3D numerical models of representative volume elements with different volume fractions have been generated and studied. The influence volume fraction of carbon particles is examined on the effective electrical conductivity, and experimental and analytical estimations for Nickel foam were also used to compare their results with those of the numerical method.
Methodology
After generating the models, the commercial FE COMSOL Multiphysics is used for the simulations, see the computing process (right), governing equations for each physics separately presented as follows:
Equations:
Fluid dynamics:
Continuity: ; Momentum:
Electric current:
;
Validation
The nickel foam structure is simulated, and effective properties were compared with Bruggeman and Catalog details, there is a good agreement with simulation results.
Effective electrical conductivity
Fluid dynamic
1e-16 [A /m2]
+
-
3 [v]
0 [v]
0
1
1.5
2
2.5
3
0.5
Results
A numerical simulation of a model which includes carbon particles was performed to understand its behavior. We simulate two coupled physics in this study, including fluid dynamics and electric current. Three different models are shown in Figure 3a, Figure 1b shows the velocity and streamlines for models, and Figure 1c shows the electrical current density distribution inside each model. Detailed results for each configuration are presented below the figures. By increasing the volume fraction of solid particles, the electrical conductivity is increased. However, the porosity and permeability of the solid particles are decreased, which means the availability of reactant flow to active surfaces is limited.
Predictive, Multiphysics simulation of effective electrical conductivity, permeability,
porosity, and specific active area of Gas Diffusion Electrode microstructure
ID46